# ACADEMIC PUBLISHING & RESEARCH ANALYSIS

# Research Summary

Article		: An in-depth analysis of nucleation and growth mechanism of CdS thin film synthesized by chemical bath deposition (CBD) technique

Journal		: Scientific Reports

Year			: 2022

DOI			: 10.1038/s41598-022-19340-z

Prepared by	: Shreyas Shriwastav

### Research Objective

The study investigates the response mechanism associated with the formation of CdS thin films using a hybrid linker-assisted chemical bath deposition approach, and examines how the modified synthesis affects their optical, structural, morphological and electrical properties.

### Research Problem

- Existing Challenge:

Minimising of spontaneous aggregation of metal nanoparticles during the synthesis process of thin films

- Limitation in previous approaches:

The Chemical Bath Deposition (CBD) process of creating thin films produced aggregation in most cases

- Why the authors propose their approach:

Modifying the CBD process by introducing bi-functional linker molecules that get attached to the metal nanoparticles and avoid aggregation, thus stabilising the surface of the thin films

### Materials Studied

Substrate			:  Soda-lime glass slide substrates

Cadmium source		:  Cadmium Sulphate (CdSO₄)

Sulphur source		:  Thiourea (SC(NH2)2)

Doping-related material	:  Silver Nitrate (AgNO₃)

Linker/stabilising material	:  3-Mercaptopropionic Acid (MPA)

pH adjustment		:  Potassium hydroxide (KOH)

Other important chemicals	:  Deionized water, Methanol, Ammonium hydroxide

### Experimental Method

Step 1: Preparation of stock solutions and chemical bath

- Silver Nitrate (AgNO3) was dissolved in deionized water (50 ml) to form a 0.01 M silver nitrate solution for the preparation of Ag-doped CdS thin films.

- MPA stock solution was made by dissolving MPA (0.212 g, 2 mmol) in mixture of (10 ml methanol + 3 ml water). KOH was used to adjust the pH of the solution to 10.

- The chemical bath was prepared with deionized water and a solution of ammonium hydroxide by volume (10:1 v/v). Thiourea (0.002 M) and Cadmium Sulphate (0.002 M) were used as sources for sulphur and cadmium salts respectively.

Step 2: Synthesis of CdS thin films without MPA

- CdS: Created using the standard process of chemical bath deposition

- Ag + CdS: AgNO3 (0.8 ml of 0.01 M stock solution) was slowly added to the CdSO4 solution in a growth beaker

Step 3: Synthesis of CdS thin films mixed with MPA

- MPA + CdS: 0.1 M of MPA stock solution was added in a growth beaker 20 min after the synthesis of CdS

- MPA + Ag + CdS: AgNO₃ was added to the CdSO₄ solution. Then, MPA (0.1 M) was added to the mixture 20 min after the initiation of the complete reaction

- The addition of MPA 20 min after initiation of the reaction encouraged the optimisation of the growth mechanisms of CdS thin films

Final deposition conditions

- All mixtures were constantly and vigorously stirred for 30 min at 80 °C

### Characterization Techniques

| Technique | What it was used to examine |
| --- | --- |
| UV/Vis/NIR spectroscopy | Optical properties |
| XRD | Crystal structure |
| FESEM | Film morphology |
| EDX | Elemental composition |
| AFM | Surface topography |
| Hall Effect measurement | Electrical characteristics |

### Key Variables

Table A – Experimental Variables

| Independent variable | Conditions studied | Properties measured/affected |
| --- | --- | --- |
| Film composition | CdS CdS + Ag CdS + MPA CdS + Ag + MPA | Optical properties (Absorbance, Bandgap, Urbach energy) Structural parameters (Crystallite size, Lattice strain) Morphological and topographical characteristics (Grain size, Surface roughness) |
| Annealing temperature | As deposited* 150°C* 250°C* 350°C* 450°C* | Electrical properties (Bulk concentration, Carrier mobility, Resistivity) |

*for each of the four film compositions

Table B – Controlled Experimental Conditions

| Controlled condition | Setting |
| --- | --- |
| Deposition temperature | 80°C |
| Deposition time | 30 min |
| pH | 10 |
| Stirring | Vigorous and constant |
| Substrate | Soda-lime glass |

### Major Findings

Optical Findings

- The authors noted that CdS + MPA and CdS + Ag + MPA showed improvement with respect to the absorption potential in the visible light range compared to pure CdS. Whereas, CdS + Ag displayed the lowest absorption potential.

- The reported bandgap varied from 2.26 to 2.52 eV across the four film formulations, with CdS + MPA showing the highest value and CdS + Ag the lowest. Urbach energy varied inversely, with the lowest value reported for CdS + MPA and the highest for CdS + Ag.

Structural Findings

- XRD analysis indicated that the CdS thin films exhibited cubic and hexagonal wurtzite crystal phases. The authors reported preferred orientation along the (111/002) reflection, while the observed diffraction behaviour varied among the different film compositions.

- Also, lower lattice strain values corresponded to higher crystallite size numbers.

Morphological and AFM Findings

- FESEM analysis showed differences in surface morphology among the film formulations. The MPA-containing films exhibited reduced grain-boundary/defect features, while the mean thickness of the mixed films was approximately 70 nm.

- AFM 2-D and 3-D revealed nanoscale granular surfaces across the CdS thin-film samples, with the average surface roughness ranging from 4 to 24.3 nm. The CdS + MPA sample exhibited relatively uniform, closely distributed grains and an average roughness of 7.4 nm, while the combined CdS + Ag + MPA sample had the lowest measured average roughness at 4 nm.

Electrical Findings

- Hall-effect measurements showed that annealing altered the electrical characteristics of the CdS thin films. The study evaluated the films at temperatures ranging from as-deposited conditions to 450°C and examined carrier concentration, carrier mobility and resistivity.

- Annealing produced composition-dependent changes in electrical properties. The CdS + MPA film showed a particularly large increase in reported carrier concentration at 150°C, reaching 3.65 × 10¹⁸ cm⁻³, while its reported resistivity fell to 1.81 Ω cm.

### Conclusion

- The study developed a linker-assisted chemical bath deposition approach for synthesising CdS thin films and investigated how the modified growth process influenced their optical, structural, morphological and electrical properties.

- The prepared films showed variation in bandgap and crystal structure, while the CdS + MPA sample exhibited relatively uniform morphology and annealing produced substantial changes in the electrical characteristics of the films.

- The authors concluded that MPA, acting as both a linker and an additional sulphur source, helped regulate CdS formation and that the modified approach could support improved charge-carrier transport.

### Scope and Open Questions

The article does not provide a separate formal limitations section. Based on the experimental scope reported by the authors, several areas remain open for further investigation.

- Processing conditions	: The reported synthesis was conducted under specific conditions, including a deposition temperature of 80 °C, a deposition time of 30 minutes and pH 10. Further investigation could examine how systematic changes in these parameters affect CdS film properties.

- Generalisability	: The study focuses on CdS thin films prepared using specific combinations of Ag and MPA. Further research could investigate whether the proposed linker-assisted approach can be extended to other semiconductor or metal-chalcogenide systems.

- Data access		: The authors state that the datasets used and analysed are available from the corresponding author on reasonable request. Wider availability of the underlying data could facilitate independent re-analysis and additional comparisons.